## Slide 1: Future Photon Initiative Center for Detectors Sensors and Detectors for Physical and Chemical Sciences
Don Figer
College of Science, Professor
Future Photon Initiative, Director
Center for Detectors, Director
October 29, 2025

## Slide 2: Outline
Speaker Bio
Future Photon Initiative
Center for Detectors
CMOS Imaging Detectors for Space

## Slide 3: Don Figer - Speaker Bio
Professor in College of Science at RIT
Professor in Astrophysical Sciences and Technology Graduate Program
Director of the Center for Detectors
Director of the Future Photon Initiative
At RIT since 2006
Previously
  Space Telescope Science Institute (operates Hubble and JWST)
  UCLA (designed optics for infrared spectrograph on Keck)
Research Interests: Detectors, Massive Stars, Massive Star Clusters, Galactic Center

## Slide 4: CMOS Imaging Detectors

## Slide 5: Advancing Radiation-Tolerant CMOS Detectors for NASA Missions
Strategic Astrophysics Technology 2022: 80NSSC24K0372
Early Stage Innovations 2023: 80NSSC24K0279
PI: Don Figer

## Slide 6: Life in the Universe

## Slide 7: State of the Art Detector Candidates for Future Missions
challenging requirements for UV/O/IR observations
single-photon sensing
low dark current
near-zero read noise
multiple candidate detector technologies
CMOS: 9.4 Mpix
BAE HWK4123
SNSPD: 0.4 Mpix (Adam McCaughan/NIST)
SPAD: Pi Imaging SPAD 5122 (Antolovic et al. 2022)
EMCCD: Teledyne e2v CCD351-00
CMOS: 163 Mpix QIS (Ma et al. 2022)
Skipper CCD: 3.5 Mpix (SENSEI Collaboration)
CMOS: Teledyne e2v CIS301/302
MKID: 20 kpix (Mazin Lab, Breckenridge 2021)

## Slide 8: Single Photon Sensitivity
low-capacitance floating diffusion sense node
high-gain response of >320 μV/e-
exceeds electronics read noise
correlated double/multiple sampling
discrete photoelectron peaks
Ma, J. et al. Ultra-high-resolution quanta image sensor with reliable photon-number-resolving and high dynamic range capabilities. Sci Rep 12, 13869 (2022). https://doi.org/10.1038/s41598-022-17952-z

## Slide 9: Single Photon Detector Operation

## Slide 10: Single-Photon CMOS Image Sensors
QIS CMOS
1 Megapixel Sensors
1.1 μm pixels
HWK4123
9.4 Megapixel
4.6 μm pixels
ORCA-QUEST
HWK4123

## Slide 11: Single Photon Images
e-
e-
e-
e-
e-
e-
e-
e-

## Slide 12: Sensor Parameters and Performance
Sensor Parameters |  |  | 
Parameter | Unit | QISSAT1-2 | HWK4123
Format | - | 1024 × 1024 | 4096 × 2304
Pixel Size | μm | 1.1 | 4.6
Sensor Performance Metrics |  |  | 
Dark Current | e-/pix/s | 0.0004 (253 K) | 0.006 (233 K)
Quantum Efficiency | % (325 nm) | 35 | 60
 | % (500 nm) | 83 | 87
 | % (940 nm) | 7 | 36
Read Noise (median) | e- | 0.27 | 0.23
Full Well Depth | e- | 275 | 7000
Fill Factor | % | 100 | 100
Frame Rate | fps | up to 30 | up to 120
Current TRL | - | 5 (pixels) 4 (ROIC) | 4

## Slide 13: Radiation Mitigation Readout Modes
create and validate single event upset mitigation readout modes
develop and test damage mitigation operational modes
leverage CMOS digital pixel multiplexing
generate modular waveforms for custom readout
verify performance of custom modes at radiation beam line
advance new readout modes beyond TRL2

## Slide 14: Custom Cryogenic and Vacuum Safe Readout Electronics

## Slide 15: Detector Mounted for Radiation (left) and Optical (right) Testing

## Slide 16: Dewar and Detector at the Proton Radiation Testing Facility

## Slide 17: Integrated Dark Signal as a Function of Radiation Dose

## Slide 18: Dark Current After Irradiation
Doubling Temperature =~8.5K

## Slide 19: Single-Photon Sensing NIR Photodiode
develop Si TCAD model of pixel using Synopsys Sentaurus
demonstrate pixel operation and low-capacitance sense node
migrate structure to MCT material platform
simulate photodiode performance and compare to Si predecessor
advance single-photon sensing and photon-number resoling NIR photodiode beyond TRL2

## Slide 20: Telescopes at UofR’s Observatory (left) and RIT’s Observatory (right)

## Slide 21: Image of Lunar Terminator and Saturn
Gallagher, J., Buntic, L., Figer, D. F., and Deng, W. 2022, “Characterization of single-photon sensing and photon-number resolving CMOS image sensors,” SPIE Astronomical Telescopes and Instrumentation, Montreal, Paper 12191-28

## Slide 22: Raw image of M67 using QISCDK
Gallagher, J., Buntic, L., Figer, D. F., and Deng, W. 2022, “Characterization of single-photon sensing and photon-number resolving CMOS image sensors,” SPIE Astronomical Telescopes and Instrumentation, Montreal, Paper 12191-28

## Slide 23: Summary
challenging science
observe low photon flux sources
detect biosignatures on exoplanets
develop detector technologies for HWO single-photon sensing in UV, optical, and NIR
Recent Publications:
Gallagher, J. P., Buntic, L., Deng, W., Fossum, E. R., and Figer, D. F. 2024, Radiation tolerance of a single-photon counting complementary metal-oxide semiconductor image sensor, J. Astron. Telesc. Instrum. Syst. 10(3), 036003, doi: 10.1117/1.JATIS.10.3.036003.
Gallagher, J. P., Buntic, L., Alexani, E., Bouthsarath, K., and Figer, D. F. 2024, Characterizing radiation-tolerant single photon resolving CMOS detectors, Proceedings Volume 13103, X-Ray, Optical, and Infrared Detectors for Astronomy XI; 131030S, Yokohama, Japan, https://doi.org/10.1117/12.3019105.
Gallagher, J. P., Buntic, L., Figer, D. F., Deng, W. 2024, Characterization of single-photon sensing and photon-number resolving CMOS image sensors, Proc. SPIE 12191, X-Ray, Optical, and Infrared Detectors for Astronomy X, Montreal, Canada, https://doi.org/10.1117/12.2629006

## Slide 24
RIT CHIPS-Related Programs
NSF ExLENT: EMERGE-MICRO
Sponsor: NSF TIP & EDU Funding: ~$1M | 2024 – 2027
Develop a pilot pipeline for community college students through A.S. → B.S. in Microelectronic Engineering.
Hands-on cleanroom training, co-op placements, and industry-guided research.
Collaborators: MCC, FLCC, GlobalFoundries, Micron, University of Rochester evaluator.
NSF NRT: CMOS+X Graduate Training
Sponsor: NSF NRT Funding: ~$3M | 2024 – 2029
Provide graduate (M.S. & Ph.D.) fellowships (~20 doctoral) in interdisciplinary semiconductor research.
Focus areas: CMOS + AI, biomedical, optoelectronic, photonic, nanoelectronics, quantum, packaging.
Goal: Train 170+ next-gen engineers & scientists, emphasizing technical and professional development components.
NSF: UPWARDS for the Future
Sponsor: NSF | (UW lead) Funding: ~$10M | 2023 – 2028
U.S.–Japan university partnership engaging six U.S. and five Japanese universities.
Activities: Student exchanges, faculty visiting programs, certification, curriculum development, focused semiconductor and memory-centric research.
Objective: Build a globally connected, skilled microelectronics workforce aligned with industry needs.
DoC: BRIDGE for Microelectronics
Sponsor: Dept of Commerce/NIST CHIPS Act Funding: ~$1.5M | 2025 – 2027
Build graduate education program to train 555 students across bachelor’s, master’s, and certificate tracks in microelectronics.
Includes new online certificate offerings, industry collaboration, and student support.
Part of NSTC Workforce Partner Alliance under CHIPS Act, scaling semiconductor workforce ecosystem.
Industry Partners: Micron, GlobalFoundries, Northrop Grumman

## Slide 25
RIT CHIPS-Related Programs
NSF ExLENT: EMERGE-MICRO
Sponsor: NSF TIP & EDU Funding: ~$1M | 2024 – 2027
Develop a pilot pipeline for community college students through A.S. → B.S. in Microelectronic Engineering.
Hands-on cleanroom training, co-op placements, and industry-guided research.
Collaborators: MCC, FLCC, GlobalFoundries, Micron, University of Rochester evaluator.
NSF NRT: CMOS+X Graduate Training
Sponsor: NSF NRT Funding: ~$3M | 2024 – 2029
Provide graduate (M.S. & Ph.D.) fellowships (~20 doctoral) in interdisciplinary semiconductor research.
Focus areas: CMOS + AI, biomedical, optoelectronic, photonic, nanoelectronics, quantum, packaging.
Goal: Train 170+ next-gen engineers & scientists, emphasizing technical and professional development components.
NSF: UPWARDS for the Future
Sponsor: NSF | (UW lead) Funding: ~$10M | 2023 – 2028
U.S.–Japan university partnership engaging six U.S. and five Japanese universities.
Activities: Student exchanges, faculty visiting programs, certification, curriculum development, focused semiconductor and memory-centric research.
Objective: Build a globally connected, skilled microelectronics workforce aligned with industry needs.
DoC: BRIDGE for Microelectronics
Sponsor: Dept of Commerce/NIST CHIPS Act Funding: ~$1.5M | 2025 – 2027
Build graduate education program to train 555 students across bachelor’s, master’s, and certificate tracks in microelectronics.
Includes new online certificate offerings, industry collaboration, and student support.
Part of NSTC Workforce Partner Alliance under CHIPS Act, scaling semiconductor workforce ecosystem.
Industry Partners: Micron, GlobalFoundries, Northrop Grumman

## Slide 26: RIT-CHIPS News
This list includes NSF public records and RIT/local news releases about our CHIPS-related workforce efforts here:
NSF ExLENT:
  https://nsf.elsevierpure.com/en/projects/beginnings-empowering-minds-through-experiential-learning-researc
  https://www.rit.edu/news/rit-expands-its-workforce-initiatives-semiconductor-industry
NSF NRT:
  https://www.nsf.gov/awardsearch/showAward?AWD_ID=2345983&HistoricalAwards=false
  https://www.rit.edu/news/nsf-awards-rit-nearly-3-million-advance-semiconductor-technologies
NSF UPWARDS for the Future:
  https://nsf.elsevierpure.com/en/projects/us-japan-university-partnership-for-workforce-advancement-and-res
  https://www.rochesterfirst.com/development/inside-upwards-at-rit-an-international-semiconductor-education-exchange-program/
Department of Commerce BRIDGE for Microelectronics Program:
  https://www.nist.gov/chips/rochester-institute-technology-rit-rochester
  https://www.nist.gov/news-events/news/2024/09/biden-harris-administration-launches-nstc-workforce-center-excellence
  https://www.rochesterfirst.com/news/local-news/rit-awarded-1-5-million-to-train-555-students-in-semiconductor-program/
You can find a full list of RIT CHIPS news here: https://www.rit.edu/news/semiconductor-chips

## Slide 27: Future Photon Initiative

## Slide 28: Future Photon Initiative
The Future Photon Initiative develops photonic devices in pursuit of answers to grand questions, leveraging efforts of existing RIT research groups using the generation, transmission, manipulation, absorption, and detection of photons.
FPI cross-disciplinary teams collaborate with external university groups, industry, and national laboratories to develop new photonic device technology.
Areas include solar energy, biophotonics, high performance imaging, astrophysics, quantum, and communication.
Eight groups: Center for Detectors, Integrated Photonics Group, Nanolithography Research Lab, NanoPower Research Labs, Photonic Systems Lab, Photonics and Optics Workforce Education Research, Semiconductor Nanofabrication Lab, and the Simone Center for Innovation and Entrepreneurship.

## Slide 29: FPI Research Funding

## Slide 30: Center for Detectors

## Slide 31
CfD designs, develops, and implements photon devices to enable scientific discoveries. | CfD trains students through research and development in detectors, instrumentation, observational astrophysics, nanostructures, silicon photonics, quantum optics and photonics, and wide bandgap materials. | The CfD was established in 2010, and includes seven professors and over two dozen students at all levels of matriculation. | Staff and student researchers investigate high impact engineering and development problems through external financial support from federal agencies, private foundations, national laboratories, and industry. | The CfD operates nine laboratories in three buildings and has an average of 32 externally funded projects (~$2.5M/year).
Center for Detectors

## Slide 32
The RIT Integrated Photonics Group conducts research in the Lobozzo Photonics and Optical Characterization lab. | Dr. Preble and his team develop high performance nanophotonic devices and systems using complementary metal-oxide-semiconductor compatible materials and processes. | Their work enables unique performance and efficiency by leveraging the inherently high bandwidths and low power of photons with the intelligence of electronics.
Integrated Photonics Group

## Slide 33
The Suborbital Astrophysics Laboratory designs, integrates, and launches sounding rocket payloads for astrophysical science. | It includes clean facilities to allow disassembly and assembly of rocket instruments, optical and electronic development and validation instruments, and cryogenic and vacuum capabilities. | In this lab, Dr. Zemcov and his team prepared the CSTARS and CIBER-2 payloads for flight at White Sands Missile Range, NM.
Suborbital Astrophysics Lab