## Slide 1: The SATIN Infrared Detector Development Program and the Road to HELLSTAR
Donald F. Figer,a Justin P. Gallagher,a Lazar Buntic,a Jon Getty,b Stefan Lauxtermann,c
aCenter for Detectors, Rochester Institute of Technology, Rochester, NY
bRaytheon Vision Systems, 75 Coromar Dr., Goleta, CA 93117
cSensor Creations Inc., 5251 Verdugo Way, Suite I, Camarillo, CA 93012

## Slide 2: Outline
The SATIN program
Detector characterization
The road to HELLSTAR

## Slide 3: SATIN DETECTOR DEVELOPMENT PROGRAM

## Slide 4: SATIN
SATIN is the Short-wave infrared Advanced Technologies and Instrumentation program for NASA and NSF.
The aim is to develop large-format infrared detectors for astrophysics using HgCdTe grown on silicon substrates.
RVS designed and fabricated the devices, while the CfD characterized them.
We used the VIRGO ROIC as a test vehicle.
SATIN is now complete.
We are on the road to HELLSTAR (HgCdTe Extremely Large Layout Sensor Technology for Astrophysics Research).

## Slide 5: Table of SATIN Detectors

## Slide 6: Variable Unit Cell Design (VUC)

## Slide 7: Detector Package

## Slide 8: DETECTOR CHARACTERIZATION

## Slide 9: Linearity, Well Size, Conversion Gain

## Slide 10: Flat Field

## Slide 11: Simulated Star Field

## Slide 12: Crosstalk (3 by 3 pixel grid)

## Slide 13: Read Noise

## Slide 14: Quantum Efficiency

## Slide 15: Persistence

## Slide 16: Dark Current

## Slide 17: the road to hellstar

## Slide 18: Requirements
Table 3. The table shows HELLSTAR goals compared to SATIN performance. |  | 
Parameter | SATIN Performance | HELLSTAR Goals
Format | 1K×1K and 2K×2K | 4K×6K
Pixel Size (µm) | 20 | 10
Read Noise (e- CDS) | 27 | 20
Wavelength Range (µm) | 0.8 – 2.55 | 0.8 – 2.65
Dark Current (e-/s/pixel)* | 0.5 @ 70 (95% Operability) | 0.1
Minimum readout time (s) | 0.3 | 1
Well size (e-) | 400,000 | 300,000
Peak QE (w/AR coating) | >90% | >70% in K-band
Persistence (after 100% saturation) | <0.1% | <0.1%

## Slide 19: ROIC

## Slide 20: Cryoscope

## Slide 21: Summary
RIT and RVS developed new infrared detectors for astrophysics applications.
The CfD demonstrated high performance for these detectors.
The team, along with SCI, will now develop HELLSTAR, a 4K×6K infrared detector.
The first application is Cryoscope at the South Pole.

## Slide 22: Current* and Past Project Personnel
Donald F. Figer*
Tre Dipassio
Justin Gallagher*
Austin Ford
Valerie Fleischauer
Neil Guertin
Brandon Hanold
John Hatakeyama
Joong Lee
Michael Kha
Lazar Buntic*
Gabrielle Picher
FINESST!!!

## Slide 23: backup

## Slide 24: Dark Current of VIRGO Devices